## Slide 1: Investigating the physics behind the different performance of negative ion sources for fusion in hydrogen and deuterium
J. Rubin, D. Wünderlich, U. Fantz

## Slide 2: Neutral Beam Injectors for ITER
HNB 1
HNB 2
HNB 3
DNB
Hemsworth et al, New Journal of Physics, 2017, doi: https://doi.org/10.1088/1367-2630/19/2/025005
R. S. Hemsworth and D. Boilson, Fusion Energy. IntechOpen, 2020.doi:10.5772/intechopen.88724.
R. S. Hemsworth and T. Inoue, IEEE Trans. Plasma Sci. 33(6), 1799 (2005). doi:10.1109/TPS.2005.860090
16.7 MW / HNB, in the form of … 870 keV H0 beam for 1000 s 1 MeV D0 beam for 3600 s

## Slide 3: Negative ion sources for ITER
x4
x2

## Slide 4: Negative ion sources for ITER
Uacc
Uext
ITER requirements | H | D
Pulse length | 1000 s | 3600 s
Extracted current density | 329 A/m2 | 286 A/m2
Electron to ion current density ratio | < 1 | 
Source performance strongly limited by co-extracted electrons  Worse in Deuterium
The aim of the thesis is to deepen the understanding of this isotope effect.
Surface production : H + esurface  H-, Hx++2esurface  H- + Hx-1

## Slide 5: (Some) Diagnostics in ELISE
Drivers
Expansion
Grid system
Bias plate
Plasma grid

## Slide 6: (Some) Diagnostics in ELISE
TOP
BOTTOM
  Current Measurements  extracted negative ion current Iext, co-extracted electron current Ie
  Langmuir Probes  plasma potential Vpl, positive ion density ni, electron density ne, electron temperature Te
  Tunable Diode Laser Absorption Spectroscopy (TDLAS)  neutral caesium density nCs
  Cavity Ring-Down Spectroscopy (CRDS)  negative ion density nH-

## Slide 7: Long pulses with continuous extraction at ELISE : Iext, Ie
ITER current requirements : proven in H*, lot of improvement necessary in D
DEUTERIUM
HYDROGEN
Iext
Iext
Ietop
Iebottom
Iebottom
Ietop
PRF = 45 kW/driver
PRF = 75 kW/driver

## Slide 8: Long pulses with continuous extraction at ELISE : nCs
nCs decreases over time : 2 steps, more pronounced in D. nCsD >> nCsH and is more top/bottom uniform
DEUTERIUM
HYDROGEN

## Slide 9: Long pulses with continuous extraction at ELISE : nH-
nH- decreases over time : 2 steps, more pronounced in D. nD- ≥ nH- and is more top/bottom uniform
DEUTERIUM
HYDROGEN

## Slide 10: Long pulses with continuous extraction at ELISE : Vpl, Δϕ
ΔV decreases over time : 2 steps, more pronounced in D. ΔVD >> ΔVH and is more top/bottom uniform
DEUTERIUM
HYDROGEN

## Slide 11: Understanding the increase of Ie
Measured during the pulse @ BUG and ELISE
Measured after the pulse @ BUG
Not accessible (also nCs+, meniscus, virtual cathode), hopefully results from codes such as CsFlow3D and ONIX
Experimentally one can try to influence 2 parameters within a pulse …  caesiation  sheath potential structure Next : some examples of what could be achieved !
↓ nCs
↓ ГCs
↑ WF
↓ ГH-
↑ ne/nH-
↑Vpl, ↓ΔV
↑ Ie

## Slide 12: Mitigating the increase of Ie : improved Cs distribution at BUG
Stable amount of Cs  stable co-extracted electron current
H
D
Cs oven
Bias plate
Plasma grid
Shower
H
D
Large asymmetry

## Slide 13: Mitigating the increase of Ie : surface biasing
Electron fence  highlight connection ΔV – Ie but can not conclude (yet) it is a suitable solution
Bias plate
Plasma grid
Fence
H
D

## Slide 14
Summary
Outlook
  Compiled a detailed list of similarities/differences between H and D operation by gathering extensive diagnostics data across different machines and campaigns (shown here for long pulses with CW extraction @ ELISE)
  Formulation of a working hypothesis explaining the increase of Ie
  Dedicated campaigns have been conducted to test the hypothesis, to try to stabilize and minimize Ie (Cs shower, electron fence, various biasing configurations, …)
  Deploy work function measurements at ELISE.
  Explore new biasing strategies (flexibility with rods, BP, PG, fence)
  Work on Cs (re-)distribution (shower, one driver operation)
  Focus on plasma – beam correlations
  Integrate modelling results
   Systematic investigations in H and D

## Slide 15: Investigating the physics behind the different performance of negative ion sources for fusion in hydrogen and deuterium

## Slide 16: Back-up slides

## Slide 17: Static effect due to higher mass of Deuterium : lower diffusion

## Slide 18: WF measurements at BUG
Similar low work function reachable in both H and D  To be brought @ ELISE
Ring electrode collects photoelectrons
Pico-ammeter measures photocurrent
Measurements only possible during plasma-off phases
A. Heiler et al, SOFT 2024
A
50 V

## Slide 19: Mitigating the increase of Ie : surface biasing
Bias plate configuration has limited influence on Ie in H. Similar in D ?
Courtesy of D. Yordanov

## Slide 20: Mitigating the non-uniformity of Ie : surface biasing
Metallic rods in ELISE help symmetrizing the plasma both in H and D
2017 – 2020
2023 - present
DEUTERIUM
HYDROGEN
Time
Time
Time
Time
Time
Time

## Slide 21: Beam divergence and uniformity
Divergence is lower in D – Uniformity/Homogeneity may differ