## Slide 1: Divertor concept development for the W7-X stellarator experiment
D. Naujoks1, A. Kharwandikar1, V. Haak1, T. Sieber1, M. Banduch1, J. Boscary2, Chr. Day3, C.P. Dhard1, G. Ehrke1, J. Fellinger1, Y. Feng1, Y. Gao1, J. Geiger1, Yu. Igitkhanov3, M. Jakubowski1, R. König1, T. Kremeyer1, R. Neu2, G. Schlisio1, H. Strobel3, T. Sunn Pedersen1, Chr. Tantos3, J. Tretter1, S. Varoutis3 and the W7-X Team*
1Max-Planck-Institut für Plasmaphysik, D-17491 Greifswald, Germany
2Max-Planck-Institut für Plasmaphysik, D-85748 Garching, Germany
3Karlsruhe Institute of Technology (KIT), Institute of Technical Physics, Vacuum Department, Karlsruhe, Germany
*The full list of W7-X team members is given in T. Sunn Pedersen et al 2022 Nucl. Fusion 62 042022

## Slide 2: W7-X divertor setup OP3
optimization objectives
optimization criteria
optimization tools
physics
technology

## Slide 3: W7-X divertor setup OP3 – physical optimization objectives
power
exhaust
particle removal
impurity control
heat loads on PFCs should not exceed their specific, defined limits
  acceptable peak loads,
  tolerable input energies to individual components,
  by broadening of heat load distribution (larger wetted areas),
avoid localized excess heat loads (leading edges, fast particles).
to pump helium, the fuel gases are pumped at almost the same rate!
high neutral gas pressure in the sub-divertor region (TMPs, cryopumps)
by ensuring a high neutral gas pressure above the targets
(high ion influx into divertor plasma, efficient plugging/baffling, reduced leakages
into main chamber, optimum pumping gap area, improved guidance of the
neutrals towards the pumping positions).
acceptable net erosion
screening/retention of impurities in divertor plasma
  increase power dissipation in the divertor plasma/SOL (by seeding),
  prevent core radiation losses -> exhaust of impurities
  by friction, electric thermal forces, drift effects; reduce sputtering.


## Slide 4: W7-X divertor setup OP3 – technical optimization objectives
power
exhaust
particle removal
impurity control
heat loads on PFCs should not exceed their specific, defined limits
avoid localized excess heat loads (leading edges, fast particles)
cost reduction and limitation of production time
  reduced number of target elements/cooling circuits, i.e. aggregation of target elements into few modules
  volume production of common and flat tungsten mosaic tiles with optimized number and dimensions avoiding leading edges
  reduced material removal of flat tiles to comply with 3D surface
  optimization of bonding technology between W, Cu-OFE, CuCrZr and SS
high neutral gas pressure in the sub-divertor region (TMPs, cryopumps)
  optimization of pumping gap geometry – e.g. reflection panel in the gap
  closing of gaps confining the sub-divertor region i.e. divertor closure (w/o pumping gaps)
acceptable net erosion
screening/retention of impurities in divertor plasma


## Slide 5: W7-X divertor setup OP3 – technical constraints
Geometry
Cooling water supply
Handling /
Installation
Mass per target module < ~60 kg
Size similar to OP2 divertor ~0.25 m² (400x600 mm u to 300x800 mm)
Installation tolerance: Relative between modules ~0.4 mm, absolute X mm
Fix points are Ø32 mm inlet /outlet which should be near to each other
  Additional flexible pin support to make module statically determined
12x supply line Ø32 mm with 5 l/s, static pressure 10 bar
  Limits: ΔT = ~60K, Δp = 15 bar
Nearly flat heat sinks with mosaic of flat W95NiFe tiles of max. ~40 x 40 mm
Radially curved edge tile with constant radius ≥ 15 mm
  Preferred thickness before final machining ≤ 2 mm to enable bent edge tile
Final machining of W based tiles is assumed to be done by wire erosion
  Poloidal direction to be straight or convex to allow use of a straight erosion wire
  Toroidal direction can be convex or concave
Gaps between tiles inside target module > 0.5 mm, preferably ~1.4 mm
  0.14 mm gap  leading edge 0.13 mm (@ 5° incidence angle)  heat flux limit ?
Gaps between target modules > 5 mm (thermal expansion and assembly inaccuracies)
  0.43 + ~0.4 (installation) = 0.8 mm leading edge  where allowed ?
Final tile thickness: > 0.5 mm (erosion), > X mm (Cu sputtering)

## Slide 6: W7-X divertor setup OP3 – optimization criteria
heat loads on PFCs should not exceed their specific, defined limits
avoid localized excess heat loads (leading edges, fast particles).
  p < 10 MW/m2 steady state -> GLADIS tests with 15 MW/m2
  pmax = 10 MW/m2 steady state
  Tmax (WNiFe) < 1300 °C, (OFE-Cu) < 600°C, CuCrZr < 475°C, channel < 200°C
  wetted areas > 1 m2, incidence angles < 5°
power
exhaust
particle removal
impurity control
high neutral gas pressure in the sub-divertor region (TMPs, cryopumps)
  pneutrals ~ 10-2 mbar (1 Pa); AUG: 0.5-1.5 Pa
acceptable net erosion
  net erosion rate < 0.2 nm/s  @15 y * 40 days/y * 1800s/day  0.22 mm
screening/retention of impurities in divertor plasma
  W core concentration < 2e-05

## Slide 7: W7-X divertor setup OP3 – optimization tools
power
exhaust
particle removal
impurity control
heat loads on PFCs should not exceed their specific, defined limits
  fast tools: EMC3-Lite, SHFP model (-> Amit Kharwandikar / Thierry Kremeyer)
  state-of-the-art: EMC3/Eirene (-> Dieter Boeyaert / Amit Kharwandikar)
avoid localized excess heat loads (leading edges, fast particles).
  fast tools: EMC3-Lite, ANSYS (-> Antara Menzel-Barbara)
high neutral gas pressure in the sub-divertor region (TMPs, cryopumps)
  fast tools: multi-chamber models, ANSYS (-> Victoria Haak)
  fast tools: 2D-analytical model (-> Thierry Kremeyer)
  fast tools: COMSOL (molecular flow module) (-> Thierry Kremeyer)
  fast tools: Direct Simulation Monte Carlo (DSMC) (-> Amit Kharwandikar ?)
  state-of-the-art: EMC3/Eirene (-> D. Boeyaert / A.Kharwandikar)
  state-of-the-art: DIVGAS (-> Stylianos Varoutis, Christos Tantos (KIT))
  but only in the sub-divertor region
acceptable net erosion
  state-of-the-art: ERO2.0 (-> FZ Jülich (A. Kirschner, J. Romazanov))
screening/retention of impurities in divertor plasma
  state-of-the-art: EMC3/Eirene, ERO2.0 (-> Victoria Winters)
design tools -> next slide

## Slide 8: W7-X design tools with CATIA – for modified geometries
detailed CAD geometry of one divertor unit
reduced grid model with limited number of grid points
the modeling activities are supported by the development of efficient engineering tools in a CATIA environment that process the complex 3D W7-X design data at different levels of sophistication to promote an efficient interchange with the physics-based codes
the grid model [T. Sieber]