## Slide 1: TM5h1 limits in OP2
Joris Fellinger

## Slide 2: Objective
Determination of limit loads of TM5h and TM6h
    Keep TCuCrZr below 500 °C
    Keep cyclic strain range in cooling pipe below 0.27 %
Approach
    Thermal-mechanical FEM Model of TM5h
    Iterate steady state limit loads until both acceptance criteria are fulfilled
        Determine cyclic strain range by appling multiple cycles until plastic strain range is stable
    Verify allowed pulse duration for higher heat loads
        Estimate pulse duration as time to reach pipe temperature of steady state limit load
        Confirm stabilized strain range fulfills acceptance criterion for this pulse duration

## Slide 3: Modelling
Merging pipes to heat sink with extra layer braze to obtain continuous mesh
    Mesh refinement towards end of braze, 1 element over pipe thickness

## Slide 4: Thermal model
Thermal model (linear elements)
    Thermal conductance between heat sink and supports: 1 kW/m²K
    Cooling water heat transfer coefficient for TM5-6h to water of 25 °C
        25-30 kW/m²K between 20 and 200°C
    Radiation from graphite to the environment of 25 °C
    Heat load:
        100 kW/m² over whole plasma facing surface
        + X MW/m² strike line load in 7 regions

## Slide 5: Assumed heat load regions
Radiation: 100 kW/m²
Strike line region 1: X MW/m²
Strike line region 2b: X MW/m²
Strike line region 5: X MW/m²
Strike line region 4b: X MW/m²
Strike line region 2a: X MW/m²
Strike line region 3: X MW/m²
Strike line region 4a: X MW/m²
7 cases: 100 kW/m² radiation on all plasma exposed surfaces + X MW/m² in one of seven strike line regions

## Slide 6: Mechanical model
Mechanical model (quadratic elements, mesh identical to thermal model)
    Graphite and sigraflex excluded
    Bolt modelling between heat sink and support bars
        Removing bolts and holes to reduce number of elements
        Adding 2 reference points at intersection of axis bolt with contact surface of heat sink – support
          Distributed coupling between point 1 and contact surface of support, influence radius 5 mm
          Distributed coupling between point 2 and contact surface of heat sink, influence radius 5 mm
        Adding equations between point 1 and 2 to make displacements and rotations equal
          Displacement in bolt axis direction (local z) for all bolts
          Displacement in support bar direction (local y) for all bolts / Alternatively release in y direction tested once
          Displacement in pipe axis direction (local x) at 4 bolts of middle support only (red RPs)
          Rotations about local x and y axis for all bolts, rotation about local z axis remains independent
    Three point support of base plate (no restraint forces)
        ux1 = uy1 = uz1 = 0
        uy2 = uz2 = 0
        uz3 = 0
1
3
2

## Slide 7: Material properties
 | Density [kg/m³] | Thermal conductivity |  |  |  |  |  | Specific heat |  |  |  | Thermal expansion |  | Young‘s modulus | 
 |  | Temp. [°C] |  |  | [W/mK] |  |  | Temp. [°C] |  | [J/kgK] |  | Temp. [°C] | [µm/mK] | Temp. [°C] | [GPa]
Graphite | 1793 | 30. 100. 200. 300. 400. 500. 600. 700. 800. | 900. 1000. 1100. 1200. 1300. 1400. 1500. 1600. |  | 128. 144. 121. 110. 94. 88.4 81.0 73.9 69.8 |  | 63.3 59.6 54.9 51.8 49.2 46.6 44.7 42.8 | 30. 100. 200. 300. 400. 500. 600. 700. 800. | 900. 1000. 1100. 1200. 1300. 1400. 1500. 1600. | 552. 834. 954. 1140. 1270. 1430. 1510. 1590. 1680. | 1720. 1760. 1790. 1820. 1840. 1870. 1900. 1940. |  |  |  | 
CuCrZr | 8900 | 20. 50. 100. 150. 200. 250. 300. 350. 400. 450. 500. |  |  | 318 324 333 339 343 345 346 347 347 346 346 |  |  | 20. 100. 200. 300. 400. 500. 600. 700. |  | 390 398 407 417 427 437 447 458 |  | 20. 100. 200. 300. 400. 500. 600. | 16.7 17.3 17.7 18.0 18.1 18.5 18.6 | 20. 100. 200. 300. 400. 500. 600. 700. | 127 127 123 118 113 106 95 86
EN1.4404 | 7960 | 20 400 |  |  | 15 21 |  |  | 20 400 |  | 472. 520. |  | 20. 100. 200. 300. 400. 500. 600. 700. | 15.9 16.3 16.8 17.3 17.8 18.3 18.8 19.4 | 20. 100. 200. 300. 500. | 158.00 152.70 146.15 139.04 133.51
Sigraflex | 1900 | // x |  | // y |  | ┴ z |  |  |  | 500 |  |  |  |  | 
 |  | 100 |  | 100 |  | 2 |  |  |  |  |  |  |  |  | 

## Slide 8: Cyclic plastic properties: Chaboche model
 | Datatype | # back-stresses | Temp. [°C] | Yield stress fy [MPa] |  | Kinematic hardening parameter C1 [GPa] |  | Kinematic hardening parameter g1 [MPa] |  | Kinematic hardening parameter C2 [GPa] |  |  | Kinematic hardening parameter g2 [MPa] |  | Kinematic hardening parameter C3 [GPa] |  | Kinematic hardening parameter g3 [MPa] | 
EN 1.4404 [1] | Parameters | 3 | 20 100 200 300 500 | 208 204 203 94 87 |  | 22.6 5.2 9.6 40.0 18.5 |  | 562 1032 1 4750 1180 |  | 10.7 24.1 17.5 19.0 18.5 |  |  | 45 208 140 192 190 |  | 11.7 13.1 18.0 10.3 10.6 |  | 54 1 695 16 1 | 
 |  |  | Temp. [°C] | Stabilized plastic strain [%] |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | 0 | 0.1 |  | 0.2 |  | 0.3 |  | 0.4 | 0.5 |  | 0.6 |  | 0.7 |  | 0.8
CuCrZr [2] | Stabilized | 1 | 20 350 500 | 261 281 215 | 343 295 225 |  | 381 301 233 |  | 397 305 236 |  | 407 307 241 | 415 309 |  | 422 311 |  | 430 312 |  | 435
[1] Gianella, Procedia Structural Integrity 8 (2018), 318–331
[2] ITER-SDC-IV V3, Appendix A.S31.5.8

## Slide 9: Strike line heat flux limit based on TCuCrZr < 500°C
TCuCrZr = 500 °C | R1 | R2a | R2b | R3 | R4a | R4b | R5
qlimit [MW/m²] | 1.5 | 1.9 | 2 | 1.5 | 2 | 1.6 | 0.75
Tgraphite [°C] | 1294 | 1468 | 1511 | 1383 | 1478 | 1241 | 1152
Tpipe [°C] | 337 | 367 | 374 | 337 | 366 | 345 | 289
Assuming 100 kW/m² on all exposed graphite surfaces
Corresponding maximum temperatures in graphite and stainless steel pipe

## Slide 10: Graphite temperature
Radiation only
100 kW/m² + 2 MW/m² @1
100 kW/m² + 2 MW/m² @2b
100 kW/m² + 2 MW/m² @5
100 kW/m² + 2 MW/m² @4b
100 kW/m² + 2 MW/m² @2a
100 kW/m² + 2 MW/m² @3
100 kW/m² + 2 MW/m² @4a

## Slide 11: Heat loads up to TCuCrZr = 500 °C
Radiation only
100 kW/m² + 1.5 MW/m² @1
100 kW/m² + 2 MW/m² @2b
100 kW/m² + 0.8 MW/m² @5
100 kW/m² + 1.6 MW/m² @4b
100 kW/m² + 1.9 MW/m² @2a
100 kW/m² + 1.5 MW/m² @3
100 kW/m² + 2 MW/m² @4a

## Slide 12: Cyclic strain limit for stainless steel pipes
Expected W7-X cycles:
  15 years x 40 experimental days x 100 programs = 60000 cycles
  Conservative as strike line is not always on same position)
Fatigue curves from RCC-MR (2002)
  Based on cyclic tensile tests with uniform strain over the cross section  FEM strains averaged over pipe thickness (1 element)
  Δɛ calculated acc. RB3227 from local FEM peak result
    4 locations of max: ɛtotal,principle, ɛplastc,principle, ɛtplastic,eq, ɛplastic,magn
    mechanical strain components eM,ij= eTotal,ij – eThermal,ij
    strain component increments tn - tn-1: deM,ij= eM,ij,n - eM,ij,n-1
    Equivalent strain range
Criterion:
  EN1.4404  property group 3S (Tech. Annex A3)
  Strain range Δɛ < 0.27 % (Fig. A3.S3542)

## Slide 13: Example of mechanical strain history of element with max. principle plastic strain
Strain increment stable within 0.02% from 2nd loading step onwards  to be used further on

## Slide 14: Comparison strain extraction locations
 | Centroid | IP1 | IP2 | IP3 | IP4 | IP5 | IP6 | IP7 | IP8
Δε [%] | 0.20 | 0.23 | 0.15 | 0.33 | 0.18 | 0.28 | 0.13 | 0.34 | 0.10
Example case of 2 MW/m² on R2b for 29s over 2 cycles
Average strain components over pipe element
Strain components extracted at each integration point
Integration point range 0.5-1.7 x centroid value < safety margin on LCF curve

## Slide 15: Strike line heat flux limit based on ΔεEN1.4404 < 0.27%
Analyses up to steady state |  | R1 | R2a | R2b | R3 | R4a | R4b | R5
qlimit [MW/m²] @Δε = 0.27% |  | 0.5 | 0.5 | 0.6 | 0.6 | 1.0 | 0.5 | 0.3
Tpipe,max @qlimit |  | 168 | 173 | 192 | 196 | 251 | 197 | 192
Δε @ q = 0.5 MW/m² |  | 0.23 | 0.27 | 0.23 | 0.21 | 0.13 | 0.27 | 0.31
Δε @ q = 1.0 MW/m² | Y fixed |  | 0.45 | 0.44 |  | 0.23 |  | 
 | Y released |  | 0.26 |  |  |  |  | 
Δε @ q = 1.5 MW/m² |  |  | 0.60 | 0.63 | 0.64 |  |  | 
Allowed heat loads limited rather by strains in the pipe than by temperature of CuCrZr
As for baffles, allowing sliding in y-direction of the bolts would reduced significantly pipe strains

## Slide 16: Pulse duration limit for q > qlimit based onTpipe = Tmax @qlimit
Time [s] | R1 |  |  | R2a |  |  | R2b |  |  | R3 |  |  | R4a |  |  | R4b |  |  | R5 |  | 
Tlimit [°C] | 168 |  |  | 173 |  |  | 192 |  |  | 196 |  |  | 251 |  |  | 197 |  |  | 192 |  | 
 | t1 | T1max | t2 | t1 | T1max | t2 | t1 | T1max | t2 | t1 | T1max | t2 | t1 | T1max | t2 | t1 | T1max | t2 | t1 | T1max | t2
0.5 MW/m² |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 110 | 240 | 89
1.0 MW/m² | 48 | 170 | 40 | 56 | 176 | 47 | 74 | 196 | 63 | 67 | 199 | 57 |  |  |  | 79 | 200 | 68 | 75 | 241 | 46
1.5 MW/m² | 32 | 176 | 26 | 38 | 185 | 30 | 47 | 202 | 38 | 41 | 204 | 34 | 84 | 254 | 75 | 52 | 205 | 43 | 50 | 251 | 28
2 MW/m² | 25 | 180 | 20 | 31 | 195 | 23 | 37 | 211 | 29 | 31 | 206 | 25 | 58 | 259 | 50 | 41 | 212 | 33 | 39 | 256 | 21
3 MW/m² | 19 | 196 | 13 | 24 | 210 | 15 | 28 | 205 | 22 | 23 | 223 | 17 | 40 | 274 | 32 | 31 | 226 | 22 | 30 | 279 | 13
5 MW/m² | 14 | 211 | 8 | 19 | 222 | 11 | 21 | 236 | 13 | 17 | 244 | 11 | 29 | 262 | 23 | 23 | 239 | 15 | 22 | 320 | 5
1st iteration: t1 = intersection of T-t curve at Tlimit for pulse duration of 360 s (excludes overshoot)
2nd iteration: t2 = t1 - (T1max-Tlimit)/((Tlimit-T0)/t1)

## Slide 17: Confirmation of temperature and strain ranges for short pulses
Load | R1 |  |  |  | R2a |  |  |  | R2b |  |  |  | R3 |  |  |  | R4a |  |  |  | R4b |  |  |  | R5 |  |  | 
Tlimit [°C] | 168 |  |  |  | 173 |  |  |  | 192 |  |  |  | 196 |  |  |  | 251 |  |  |  | 197 |  |  |  | 192 |  |  | 
MW/m² | tpulse | Tpipe | Tsink | Δε | tpulse | Tpipe | Tsink | Δε | tpulse | Tpipe | Tsink | Δε | tpulse | Tpipe | Tsink | Δε | tpulse | Tpipe | Tsink | Δε | tpulse | Tpipe | Tsink | Δε | tpulse | Tpipe | Tsink | Δε
0.5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 89 | 183 | 299 | 0.21
1 | 40 | 161 | 240 | 0.19 | 47 | 167 | 220 | 0.22 | 63 | 187 | 233 | 0.19 | 57 | 190 | 269 | 0.20 | 68 |  |  | 0.24 | 68 | 192 | 261 | 0.24 | 46 | 197 | 329 | 0.22
1.5 | 26 | 164 | 250 | 0.19 | 30 | 168 | 220 | 0.22 | 38 | 186 | 230 | 0.19 | 34 | 191 | 272 | 0.20 | 75 48* | 248 | 308 | 0.42 0.29 | 43 | 191 | 253 | 0.24 | 28 | 185 | 316 | 0.20
2 | 20 | 167 | 260 | 0.19 | 23 | 170 | 223 | 0.23 | 29 | 189 | 213 | 0.20 | 25 | 190 | 274 | 0.20 | 50 32 | 249 | 307 | 0.42 0.28 | 33 | 194 | 252 | 0.25 | 21 | 184 | 313 | 0.20
3 | 13 | 158 | 255 | 0.19 | 15 | 148 | 214 | 0.22 | 22 | 185 | 231 | 0.22 | 17 | 193 | 280 | 0.21 | 32 20 | 252 | 287 | 0.42 0.26 | 22 | 181 | 224 | 0.25 | 13 | 170 | 293 | 0.18
5 | 8 | 155 | 253 | 0.17 | 11 | 162 | 204 | 0.25 | 13 | 182 | 225 | 0.21 | 11 | 198 | 287 | 0.21 | 23 13 | 261 | 321 | 0.47 0.26 | 15 | 194 | 239 | 0.26 | 5 | 118 | 196 | 0.11
* Pulse duration of 1.5 MW/m² needs further reduction to 43 s as for R4b

## Slide 18: Final recommendations
 |  | R1 | R2a | R2b | R3 | R4a | R4b | R5
Steady state heat load [MW/m²] |  | 0.5 | 0.5 | 0.6 | 0.6 | 0.6 | 0.6 | 0.3
Allowed pulse duration [s] | 0.5 [MW/m²] |  |  |  |  |  |  | 90
 | 1.0 [MW/m²] | 47 | 47 | 68 | 68 | 68 | 68 | 47
 | 1.5 [MW/m²] | 30 | 30 | 43 | 43 | 43 | 43 | 30
 | 2.0 [MW/m²] | 23 | 23 | 30 | 30 | 30 | 30 | 23
 | 3.0 [MW/m²] | 15 | 15 | 22 | 22 | 22 | 22 | 15
 | 5.0 [MW/m²] | 11 | 11 | 15 | 15 | 15 | 15 | 11
Regions grouped into 2 groups
100 mm
60 mm