## Slide 1: Exploration of scenarios compatible with carbon-free operation and tungsten PFCs
C.P. Dharda, D. Naujoksa, Y. Gaoa, T. Stangea, B. Buttenschöna, S. Brezinsekb, D.A. Ennisc, E. Floma, D. Gradica, D. Hartmanna, F. Henkea, M. Jakubowskia, P. Kornejewa, M. Mayerd, P. McNeelya, R. Neud and the W7-X Team
aMax-Planck-Institut für Plasmaphysik, Wendelsteinstraße 1, 17491 Greifswald, Germany
bForschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung, Plasmaphysik, 52425 Jülich, Germany
cDepartment of Physics, Auburn University, 380 Duncan Drive, Auburn, Alabama 36849, USA
dMax-Planck-Institut für Plasmaphysik, Boltzmannstr. 2, 85748 Garching, Germany

## Slide 2: Content
Deliverables
Experiment details and results
Summary:
  Main results and the status of experiments from OP2.1
  Plans for OP2.2/2.3
Deliverables:
D8: Definition of the operation limits associated with plasma-facing components containing tungsten materials
D10: Determination of erosion effects due to seeding impurities
Thanks to Marianne Richou (CEA/WEST) for providing the video
UFOs in Tore Supra with C-PFCs

## Slide 3: Tungsten plasma-facing components (PFCs) in OP2.1
  Heat shield tiles in the ECRH beam dump areas coated with tungsten (1 m2 each in modules 1 and 5)
  40 tungsten baffle tiles in module BM1v (NBI beam dump), W (in module 2), W95Cu1.5Ni3.5 in modules 1,3,4,5
  15 coated tiles at different heat shield positions
  9 tiles opposite to AAE50 spectroscopy
  16 coated tiles with special marker layers in M 1 & 5
  Laser blow-off (LBO) and TESPEL injections
  exposure of W/W-alloys with the MPM OP2.2
Ref: D Naujoks et al, PFMC (2023)

## Slide 4: Tungsten PFCs (Baffle BM1v) – geometry modifications for OP2.1
4
prediction: a factor of two is the anticipated reduction with present boundary conditions
BM1v: thin W/WCuNi tiles together with modified graphite tiles (photo taken in module 1, lower divertor with 4 WCuNi tiles in the center of this baffle module)
graphite W/WCuNi tiles graphite
TB-W049-13
tile-modification strategy for local heat load reduction: making the tiles thinner, but also reducing the local incidence angle via toroidally shifting the watershed location
modified form
Ref: D Naujoks et al, PFMC (2023), Y Gao et al 2023 Nucl. Fusion 63 026031

## Slide 5: Experiments OP1.2b (old design) with OP2.1 (new design)
5
5 MW ECRH input power
OP1.2b: https://w7x-logbook.ipp-hgw.mpg.de/log.html?id=XP_20181011.21
OP2.1: https://w7x-logbook.ipp-hgw.mpg.de/log.html?id=XP_20230328.23
PECRH ≤ 5 [MW]
ne, dl ≤ 6·1019 [m-2]
Wdia ≤ 0.45 [MJ]
Prad ≤ 1 [MW]
OP1.2b
OP1.2b
OP2.1
OP2.1
Ref: D Naujoks et al, PFMC (2023)

## Slide 6: Experiments OP1.2b (old design) with OP2.1 (new design)
6
Note: the emissivity of W is assumed to be 0.67 based on the equilibrium temperature of 50 C during the hot water test.
 | 20181011.021 (OP1.2b: 5 MW) | 20230328.023 (OP2.1: 5 MW) | 20181009.009 (OP1.2b: 3 MW) | 20230328.033 (OP2.1: 3 MW)
Mean heat load (kW/m2) | 129.66 | 81.8 | 82.8 | 47.1
Max heat flux (MW/m2) | 0.95 | 0.3 | 0.92 | 0.26
5 MW ECRH input power
OP1.2b: https://w7x-logbook.ipp-hgw.mpg.de/log.html?id=XP_20181011.21
OP2.1: https://w7x-logbook.ipp-hgw.mpg.de/log.html?id=XP_20230328.23
3 MW ECRH input power
OP1.2b: https://w7x-logbook.ipp-hgw.mpg.de/log.html?id=XP_20181009.9
OP2.1: https://w7x-logbook.ipp-hgw.mpg.de/log.html?id=XP_20230328.33
averaging over 8 baffle tiles as indicated (orange box)
reduction of heat loads by a factor 2-3
PECRH ≤ 5 [MW]
ne, dl ≤ 6·1019 [m-2]
Wdia ≤ 0.45 [MJ]
Prad ≤ 1 [MW]
PECRH ≤ 3 [MW]
ne, dl ≤ 5·1019 [m-2]
Wdia ≤ 0.4 [MJ]
Prad ≤ 0.8 [MW]
Ref: D Naujoks et al, PFMC (2023)

## Slide 7: Tungsten baffle tiles after OP2.1
7
IMG_5471/5473: Tungsten tiles in BM1v of DU29 with deposition layers flaking off
Photos: M Endler et al, W7-X Physics meeting 18.09.2023
Specific experiments were conducted in high mirror (KKM) with Ar seeding to investigate the tungsten erosion
Normal operation in standard (EJM) configuration with various seedings
No tungsten erosion was observed  If the surfaces were already covered with depositions or edge spectrometer viewing misalignment (Dorothea’s presentation), need to be addressed for OP2.2/2.3

## Slide 8: W7-X: tungsten PFCs – heat shield (ECRH beam dump, M1)
8
Video camera system (view from AEQ51, 5.5s to 6.2s) Ref: G Cseh, G Kocsis
ECRH O2-heating scenario was redesigned for OP2 to reduce stray radiation by about 50% by using special reflector tiles with polarization gratings and beam broadening
OP2.1: Density peaking much higher as expected from OP1.2b data
Stronger refraction of ECRH-beams caused hot spot with tungsten cluster/flake emission
main reflector tiles with holographic grating made of TZM
(note: the initial W coating had to be removed by glass bead blasting because it was flaking off)
adjacent tiles made of graphite with tungsten coating
Ref: D Naujoks et al, PFMC (2023)
Photo DSC_0294, M Endler

## Slide 9: Tungsten PFCs – heat shield (ECRH beam dump, Module 1)
9
Ref: M Endler et al, W7-X Physics meeting 18.09.2023
IMG_8508
High loads at few locations in module1 with melting of W-layer,
the evaluations (M Endler) show these are most likely not due the leading edges
possible causes: fast ions/electrons.

## Slide 10: Tungsten injection by TESPELs (and LBO)
10
EJM007+2520 standard conf.
TESPEL 0.65x1017 W
TESPEL 2.5x1017 W
TESPEL 1.3x1017 W
TESPEL 5.5x1017 W
calibration of core spectroscopy (HEXOS) with tungsten pellets (TESPEL)
detection limit estimated as nW/ne ~ 7.5·10-7 for ne = 4·1019 m-3, Te = 3 keV
plasma survived after an almost complete loss of energy by transition into a small plasma [XP_20230314.58] Ref: G Cseh, G Kocsis
Ref: D Naujoks et al, PFMC (2023)

## Slide 11: OP2.1: scenario development compatible with tungsten PFCs
during (normal) plasma operation in OP2.1:
- no observation in HEXOS or in the PHA system,
- no W signals in the visible range spectroscopy
MMG000+2520 (low-shear): BM1v (AEK31) up to 700 °C
W I 361.75 nm
W I 363.19 nm
W II 364.14 nm
W I 368.8 nm
W I 378.08 nm
W I 400.9 nm
Ref: D Naujoks et al, PFMC (2023)

## Slide 12: Enlarged tungsten surfaces for OP2.2/2.3
IMG_9006 from HM19
IMG_9078 from HM38
IMG_9035 from HM29
W-coated graphite tiles installed in baffle module BM1v
8 tiles in HM18/19/39/48/49/58/59
7 tiles in HM39 (one tile couldn’t be removed due to fixed TZM screw)
4 tiles in HM28/29 (4 tiles were not exchanged since these are used for the HST)

## Slide 13: Summary: Main results and the status of OP2.1 experiments
No observation of tungsten enrichment / accumulation during normal plasma operation
No tungsten erosion observed by the in-situ spectroscopy (core/edge) from the tungsten surfaces (only very limited dedicated experiments could be conducted)
  from the baffle tiles due to the plasma and impurity (seeded and intrinsic) ion impacts
  from the heat shield tiles due to the charge-exchange neutrals.
Strong tungsten erosion was observed (in-situ) on heat shield tile in module 5 due to refraction of ECRH-beam  Tile has been replaced, such ECRH operations will be avoided.
The inspection after opening the vessel showed tungsten erosions at the edge of a couple of heat shield tiles in module 5 due to leading edges  New tiles are installed with no leading edges, the reason for such excessive loads at these farther locations are under investigation, these tiles will be observed after OP2.3.
13 baffle tiles, 18 heat shield tiles (W-surfaces) and 71 neighboring baffle tiles (graphite surfaces) have been retrieved for the post-mortem analysis  followed by the ERO2.0 and WallDYNE 3D modelling.
Thicker depositions (C/B/…) prevented the tungsten erosion on the baffles  Loose flakes are being removed.
Only a few experiments could be conducted partially, edge spectroscopy had only a limited view.

## Slide 14: Summary: Plans for OP2.2/2.3
The tungsten surface area has been enlarged by installing 71 W-coated tiles in baffles BM1v.
All the partially attempted experiments need to be completed.
The experiments which could not be taken up due to the sessions being cancelled need to be conducted, including the samples exposure via the multipurpose manipulator (MPM).
All the tungsten experiments need to be planned right in the beginning of the campaign OP2.2 so that the effects due to the depositions could be avoided.
Edge-spectroscopy view to the baffle tiles has been greatly improved, thanks to installing new W-coated tiles, providing better possibilities of tungsten detection in a broader range.
X-ray imaging spectroscopy is being equipped to detect tungsten spectral lines in a wider range.
A substantial increase in the tungsten surface areas by installing larger number (e.g. 25% of the total ca. 8000 tiles after each dual campaign) of tiles would be required as a final validation step to prove the tungsten can be used in W7-X.

## Slide 15: .
Back-up slides

## Slide 16: Tungsten as plasma-facing material in fusion machines
+ High melting point, low sputtering, low activations, low fuel retention …
- High Z (core radiation), hard to machine, high cost …
Ref: W Eckstein et al, Sputtering data, IPP report 9/82, 1993, p.116